## Slide 1: Inductance in an Electro-Permanent Magnet as a proxy for Holding Force
J. Belicki
Contributions by R. Smith
2017-07-12
“…magnets, how do they work?...”

## Slide 2: Zwicky Transient Facility’s (ZTF) Need
Instrument in beam path, so beam obstruction must be kept to a minimum
Limited space within/around instrument Limited number of power and signal wires
Required: Low profile mechanism to retain filters for ZTF, high reliability, ability to detect distance/engagement of filter
Solution?

## Slide 3: Electro-Permanent Magnets!
Three magnets obstruct < 0.2% of beam
457mm
498mm
25mm

## Slide 4: What is an Electro-Permanent Magnet (EPM)?
An EPM is a permanently magnetized metal that has a coil of wire around its core
When power is supplied (24V for our magnets), a current flows through the coils and creates a magnetic field of equal (but opposite) magnitude, canceling out the magnetic field
Two wires used to supply power to EPM
  Same two wires can be used to measure plate distance and engagement!

## Slide 5: Force vs Current
Resistance is constant  Direct relationship between voltage and current at low frequencies
V = I/R
Data from J. Zimmer

## Slide 6: Force vs Distance
Force rolls off steeply with air-gap
 pickup of metal particles could compromise holding force.
 sensing of that air- gap is essential for reliability

## Slide 7: B-H curves for electromagnet
H (ampere turns)
Soft iron core with low hysteresis
Low L
Low residual magnetization with zero applied current
B (tesla)
Mild steel target plate works approximately like this

## Slide 8: Permanent magnets = high hysteresis
H (ampere turns)
B (tesla)
B field saturates at lower value than for soft iron  permanent magnet is not as strong at electromagnet
1) Magnetize by applying high current to coil to flip all dipoles to same orientation
2) Stays magnetized when current removed (dipoles stay aligned)

## Slide 9: Inductance Sensing Circuit
On to de-energize EPM,
Off when sensing.
24 V pulse

## Slide 10: L-R Circuit rise time
Vi
V0 =iR
VL=L*di/dt
Vi = VL + V0 = L*di/dt + iR
V0 = A * [1 – exp(-R*t/L) ]
A
Initially i=0, V0=0, so
VL = A = L*di/dt
di/dt = A/L
dV0/dt = A*R/L

## Slide 11: L-R Circuit rise time
Vi
V0 =iR
VL=L*di/dt
Vi = VL + V0 = L*di/dt + iR
V0 = A * [1 – exp(-R*t/L) ]
A
Inductance increases when target plate bridges air gap across permanent magnet.
Magnetic field indication paper showing magnetic field lines from EPM

## Slide 12: Measure initial rise with short pulse
Vi
V0 =iR
VL=L*di/dt
Pulse for only 1 ms, to allows signal to rise to about 10% of full value and thus only slightly offset holding force.
… but enough to pull core out of saturation (more on this later)
Input pulse, 24V
EPM Response

## Slide 13: EPM is non-Linear Inductor!!
How does hysteresis curve affect inductance?
First we need to know how does one derive inductance from “first principals.”
In fact let’s go back to the beginning of creation.
“Let there be light”….

## Slide 14: Let there be light!
Maxwell’s equations

## Slide 15: Faraday’s Law
Voltage around loop = rate of change of flux through loop
V = - dΦ/dt
v = L * d i/dt
Inductance, L is defined by the relation:
Thus
L = dΦ/di
 If flux is non linear function of current, so is inductance
Sign convention for V reversed!

## Slide 16: B-H curves for electromagnet
H (ampere turns)
Air cored solenoid
Low L
Soft iron core with low hysteresis
Low L
Low L
Slope, L=dΦ/di, is high at low current
Low residual magnetization with zero applied current
B (tesla)
When core fully saturates, slope is same as for air core.

## Slide 17: B-H curve for permanent magnet
H (ampere turns)
High L
Slope, dΦ/di=L, is low when applied current is low. Opposite of electromagnet with low hysteresis core.
High residual magnetization with zero applied current
Apply this current to offset permanent field of core. Red curve is retraced when current is removed so magnetization remains.
B (tesla)
high hysteresis
B field saturates at lower value than for soft iron  permanent magnet is not as strong at electromagnet
Avoid excess current since negative net field (B) will begin to demagnetize
Low L

## Slide 18: When air gap is bridged
H (ampere turns)
B (tesla)
Hypothesis to explain data
Both core and plate saturated ... we never go here.
Inductance increases monotonically with air gap at large excitation current
Plate in place
Narrow air gap
No plate present
Very little slope change at low current

## Slide 19: Ambiguity!

## Slide 20: Non-monotonicity hypothesis
B (tesla)
Linear segment approximation
Core saturates
H (amp-turn)
Plate air gap
Plate attached
No Plate
Plate saturates
Low slope
High slope
Med.slope

## Slide 21: More current helps, but still not monotonic
B (tesla)
Core saturates
H (amp-turn)
Plate air gap
Plate attached
No Plate
Plate saturates
Low slope
High slope
Med.slope

## Slide 22: Subtract initial reading  monotonic
B (tesla)
Core saturates
H (amp-turn)
Plate air gap
Plate attached
No Plate
Plate saturates
Low slope
Med. slope
High slope

## Slide 23: Multiple Pulse Times

## Slide 24: Breaking Ambiguity!

## Slide 25: Variations Between EPMs

## Slide 26: Variations Between EPMs: signal @1ms – signal @ 0.5ms with scaling)

## Slide 27: Variations Between EPMs: signal @1ms – signal @ 0.5ms w/o scaling)

## Slide 28: Calibrations In Progress
Variation between EPMs
Temperature dependence
Better force versus distance  force versus measured rise time.