

**Fiber Arm black coating (dry lube) rub off tests and results**

1. Rubbing with IPA – result: coating held up




1. Rubbing with Acetone – result: coating held up



1. Ultrasonic cleaning with Acetone (60C, 3 min) – result: coating held up 

Before After

1. Ultrasonic cleaning with Acetone (60C, 5 min) – result: coating held up 

Before After

1. Sand paper (1000 grid), light pressure – result: coating came off

Other side of the piece that is sanded with 1000 grid

Sanded with 1000 grid, coating came off at the tops

Never been through any test

Never been through any test